Author’s Response for Reviewer’s Comments

| Reviewer’s Comments | Author’s Response |
| --- | --- |
| Reviewer A |  |
| - It is focusing on RHA, but not mentioned in the title. | The title was changed to “Synthesis of Silica Derivative-Salen from Rice Husk and its use for Extraction of Divalent Metal Ions Co(II), Ni(II) and Cu(II)” |
| - Many aricles in IJC have reported functionalized silica. It is suggested to cite those to improve the novelty. For example: Indones. J. Chem., 2015, 15 (2), 108 – 115; ndones. J. Chem., 2017, 17 (2), 264 – 273, ect. | One of the mentioned articles was cited (Reference no 25). |
| - AFM cannot be found in characterization technique section. | AFM was added to the technique section as required. |
| - Author(s) have to provide FTIR spectra of RHA, RHACl and RHAI. | The requested spectra were added and presented in an overlay fashion. |
| - In both spectra of RHACSALEN and RHACEN appear peak around 1650 cm-1. How to ensure that peak at 1651 cm-1is belong to C=N group? | The difference in location and intensity, as well as the overlap between them |
| - How many ethylenediamine and salicylaldehyde group (mmol g-1) in the surface of RHACSALEN? | Table 1 shows the elemental analysis of the RHACSALEN and showing the increase ratio of the number of carbon, nitrogen and hydrogen atoms |
| - Author(s) is advised to provide SEM images of RHA, RHAEN and RHACSALEN | I would like to inform you that the completion of this work for a long time more than a year and most of the raw materials are not available now. |
| - RHA and RHAEN are essential to be analyzed by TGA DTA as comparison. | I would like to inform you that the completion of this work for a long time more than a year and most of the raw materials are not available now. |
| - How effectiveness of the adsorbent has to be compared to others reported previously. | The effectiveness of the adsorbent was compared to others reported previously. The comparison is presented in Table 5. |
| - In order to obtain rate of adsorption value, author(s) have to evaluate the experimental data with some kinetic model such as pseudo-1 order and pseudo-2 order. | The experimental data was evaluated with 4 kinetic models: First order, second order, pseudo first order and pseudo second order. Additionally, rate constant was calculated for each model, and the results were listed in Table 3. |
| - Experimental data need to be evaluated with some isotherm models such as Langmuir, Freundlich and/or Temkin model. Some parameter related to those models are also essential to be added in this manuscript. | The experimental data was evaluated with Langmuir and Freundlich model. The related parameters were also calculated and added to the manuscript. The results were listed in Table 4. |
| - Further explanation on why adsorption is favorable on acidic condition has to be provided by author(s). | Added in the effect of pH |
| - It is suggested to be unified by overlay. | FTIR spectra were unified by overlay as requested. |
| Editor |  |
| - Title does not represent the content; The experiment used RHA and discussed it intensively but it is not mentioned in the title. | The title was changed to “Synthesis of Silica-Salen Derivative from Rice Husk Ash and its use for Extraction of Divalent Metal Ions Co(II), Ni(II) and Cu(II)” |
| - Introduction section does not describe previous research of Cu(II), Ni(II) and Co(II). Many researches reported the adsorbent of those meta lions. | Some previous pieces of research were cited in Table 5. |
| - Many articles reporting RHA and functionalized silica. It is suggested to search and cite the relevant theme to improve the novelty. | Uptake of element ions by solid ligands from silica extracted of rice husks is a recent subject that has not been mentioned before. Yes, The ions of the elements has been estimated by references of other prepared silica and also adopted as references. |
| - Experiment data presented are not discussed comprehensively and not compared to previous reported researches, therefore the scientific contents need to be improved. | The experimental data was compared to others reported previously. The comparison is presented in Table 5. |
| - The quality of the figures in general is poor and need to be revised, especially the scale and legends too small/unclear | The quality of the figures was improved. |