Supplementary Information (SI)

SI 1:

The photoreduction of Ag (I) from radiophotography wastewater

  - Making of standard solution

| Concentrations (mg/L) | Absorbances |
| --- | --- |
| 2 4 6 8 10 | 0.071 0.139 0.193 0.254 0.310 |

  - Photoreduction of Ag+ from radiophotography wastewater catalyzed by  TiO2

| Weight of TiO2 (mg) | Initial weight of Ag in the wastewater (mg/1000 mL) | Initial weight of Ag in the 250 mL (mg/250 mL) | Residual weight of Ag in the 250 mL (mg) | Reduced weight of Ag (mg) | Weight of Ag in 1 g of catalyst (mg/g) |
| --- | --- | --- | --- | --- | --- |
| 150 300 450 | 1502.5 1502.5 1502.5 | 375.625 375.625 375.625 | 110.479 95.747 146.252 | 265.146 279.878 229.373 | 1.77 0.93 0.51 |

  - Calculation of Ag+ photoreduction from radiophotography wastewater catalyzed by TiO2

Initial concentration of Ag in the radiophotography wastewater:

y        = 0.0297x + 0.0155

0.194 = 0.0297x + 0.0155

x        = 0.17850.0297

x        = 6.01

Cs      = 6.01 x 250

= 1502.5 mg/L

So, the concentration of Ag in the 250 mL of sample is 375.625 mg/L.

TiO2 with 150 mg of weight

y        = 0.0297x + 0.0155

0.068 = 0.0297x + 0.0155

x        = 0.05250.0297

x        = 1.767

Cs      = 1.767 x 250

= 441.91 mg/L

Final weight of Ag+ = Concentration of Ag+ in the filtrate x Volume of

filtrate (L)

= 441.91 mg/L x 0.250 L

= 110.479 mg

Reduced weight of Ag = Initial weight of Ag+ – residual weight of Ag+

= 375.625 mg - 110.479 mg

= 265.146 mg

Weight of Ag in catalyst (mg/g)	=  reduced weight of Agcatalyst weight of TiO2

=  265.146 mg150 mg

=  1.77 mg

TiO2 with 300 mg of weight

y        = 0.0297x + 0.0155

0.061 = 0.0297x + 0.0155

x        = 0.04550.0297

x        = 1.532

Cs      = 1.532 x 250

= 382.99 mg/L

Final weight of Ag+ = Concentration of Ag+ in the filtrate x Volume of

filtrate (L)

= 382.99 mg/L x 0.250 L

= 95.747 mg

Reduced weight of Ag = Initial weight of Ag+ – residual weight of Ag+

= 375.625 mg – 95.747 mg

= 279.878 mg

Weight of Ag in catalyst (mg/mg)	=  reduced weight of Agcatalyst weight of TiO2

=  279.878 mg300 mg

=  0.93 mg

TiO2 with 450 mg of weight

y        = 0.0297x + 0.0155

0.085 = 0.0297x + 0.0155

x        = 0.06950.0297

x        = 2.340

Cs      = 2.340 x 250

= 585.01 mg/L

Final weight of Ag+ = Concentration of Ag+ in the filtrate x Volume of

filtrate (L)

= 585.01 mg/L x 0.250 L

= 146.252 mg

Reduced weight of Ag = Initial weight of Ag+ – residual weight of Ag+		    			  = 375.625 mg – 146.252 mg

= 229.373 mg

Weight of Ag in catalyst (mg/mg)	=  reduced weight of Agcatalyst weight of TiO2								=  229.373 mg450 mg

=  0.51 mg

SI 2: Calculation of band gap energy using edge absorption theory

2.1 Calculation result of SR-UV for TiO2 photocatalyst

Wavelength (nm)

y1 = y2

-0.02563x + 10.03489	= -4.855 x 10-4x + 0.43104

10.03489-0.43104 	= -4.855 x 10-4x + 0.02563x

9.60385			= 0.0251445x

x			= 9.603850.0251445

x 			=  381.94 nm

E (Joule) 	= h.cλ

= 6.63 x 10-34 J.s .  3 x 108m.s-13.8194 x 10-7 nm

=  1.989 x 10-25 J.s.  m.s-13.8194 x 10-7 nm

= 5.207 x 10-19 J

E (Joule)	= E(Volt)6.24151 x 1018

E (Volt) 	= 5.207 x 10-19 J . 6.24151 x 1018

= 3.25 eV

2.2 Calculation result of SR-UV for TiO2/Ag photocatalyst (150/1.767 mg)

Wavelength (nm)

y1 = y2

-0.09873x + 41.01024	= -0.00114x + 0.96307

41.01024-0.96307 	= -0.00114x + 0.09873x

40.04717			= 0.09759x

x			= 40.047170.09759

x 			=  410.36 nm

E (Joule) 	= h.cλ

= 6.63 x 10-34 J.s .  3 x 108m.s-14.1036 x 10-7 nm

=  1.989 x 10-25 J.s.  m.s-14.1036 x 10-7 nm

= 4.847 x 10-19 J

E (Joule)	= E(Volt)6.24151 x 1018

E (Volt) 	= 4.847 x 10-19 J . 6.24151 x 1018

= 3.02 eV

2.3 Calculation result of SR-UV for TiO2/Ag photocatalyst (300/0.933 mg)

Wavelength (nm)

y1 = y2

-0.07236x + 30.36066	= -0.00112x + 0.95953

30.36066 – 0.95953	= -0.00112x + 0.07236x

29.40113			= 0.07124x

x			= 29.401130.07124

x 			=  412.70 nm

E (Joule) 	= h.cλ

= 6.63 x 10-34 J.s .  3 x 108m.s-14.1270 x 10-7 nm

=  1.989 x 10-25 J.s.  m.s-14.1270 x 10-7 nm

= 4.8194.10-19 J

E (Joule)	= E(Volt)6.24151 x 1018

E (Volt) 	= 4.8194 x 10-19 J . 6.24151 x 1018

= 3.00 eV

2.4 Calculation result of SR-UV for TiO2/Ag photocatalyst (450/0.509 mg)

Wavelength (nm)

y1 = y2

-0.06838x + 27.61638	= -9.02875 x 10-4x + 0.80976

27.61638 – 0.80976	= -9.02875 x 10-4x + 0.06838x

26.80662			= 0.06747x

x			= 26.806620.06747

x 			=  397.31 nm

E (Joule) 	= h.cλ

= 6.63 x 10-34 J.s .  3 x 108m.s-13.9731 x 10-7 nm

=  1.989 x 10-25 J.s.  m.s-13.9731 x 10-7 nm

= 5.0061 x 10-19 J

E (Joule)	= E(Volt)6.24151 x 1018

E (Volt) 	= 5.0061 x 10-19 J . 6.24151 x 1018

= 3.12 eV

SI 3: Caracterization Result of XRD

3.1 Difractogram of TiO2

## Measurement Conditions:

Dataset Name	TiO2

File name	E:\DATA PENGUJIAN\Pengujian 2019\Mei\Nahzim\TiO2\TiO2.rd

Comment	Configuration=Reflection-Transmission Sp

Goniometer=PW3050/60 (Theta/Theta); Mini

Measurement Date / Time	5/9/2019 11:23:00 AM

Raw Data Origin	PHILIPS-binary (scan) (.RD)

Scan Axis	Gonio

Start Position [°2Th.]	5.0084

End Position [°2Th.]	89.9744

Step Size [°2Th.]	0.0170

Scan Step Time [s]	10.1500

Scan Type	Continuous

Offset [°2Th.]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.2500

Specimen Length [mm]	10.00

Receiving Slit Size [mm]	12.7500

Measurement Temperature [°C]	-273.15

Anode Material	Cu

K-Alpha1 [Å]	1.54060

K-Alpha2 [Å]	1.54443

K-Beta [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	30 mA. 40 kV

Diffractometer Type	XPert MPD

Diffractometer Number	1

Goniometer Radius [mm]	200.00

Dist. Focus-Diverg. Slit [mm]	91.00

Incident Beam Monochromator	No

Spinning	Yes

## Main Graphics. Analyze View:

## Peak List:

| Pos. [°2Th.] | Height [cts] | FWHM Left [°2Th.] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 25.1301 | 1575.25 | 0.2007 | 3.54376 | 100.00 |
| 27.2658 | 20.99 | 0.2007 | 3.27084 | 1.33 |
| 28.2320 | 6.70 | 0.1506 | 3.16105 | 0.43 |
| 36.7986 | 95.77 | 0.1673 | 2.44248 | 6.08 |
| 37.5962 | 334.97 | 0.0669 | 2.39247 | 21.26 |
| 38.4318 | 105.29 | 0.2007 | 2.34236 | 6.68 |
| 41.3423 | 5.10 | 0.8029 | 2.18393 | 0.32 |
| 47.8685 | 501.85 | 0.1338 | 1.90032 | 31.86 |
| 52.2461 | 2.40 | 0.1004 | 1.75093 | 0.15 |
| 53.6934 | 284.62 | 0.1171 | 1.70711 | 18.07 |
| 54.9072 | 286.25 | 0.0836 | 1.67221 | 18.17 |
| 61.9399 | 51.45 | 0.1673 | 1.49816 | 3.27 |
| 62.5450 | 227.81 | 0.1338 | 1.48512 | 14.46 |
| 68.5963 | 93.18 | 0.1338 | 1.36812 | 5.92 |
| 70.1619 | 103.65 | 0.1171 | 1.34138 | 6.58 |
| 74.8830 | 171.14 | 0.1171 | 1.26809 | 10.86 |
| 75.8810 | 36.14 | 0.1224 | 1.25284 | 2.29 |
| 80.6568 | 9.15 | 0.4015 | 1.19125 | 0.58 |
| 82.5637 | 73.51 | 0.1673 | 1.16850 | 4.67 |

3.2 Difractogram of TiO2/Ag (150/1.767 mg)

Main Graphics. Analyze View:

## Peak List:

| Pos. [°2Th.] | Height [cts] | FWHM Left [°2Th.] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 25.2678 | 866.34 | 0.2175 | 3.52475 | 100.00 |
| 27.3999 | 11.04 | 0.4015 | 3.25513 | 1.27 |
| 36.9949 | 51.26 | 0.2342 | 2.42997 | 5.92 |
| 37.7881 | 211.63 | 0.2342 | 2.38077 | 24.43 |
| 38.5505 | 69.22 | 0.2007 | 2.33542 | 7.99 |
| 47.9354 | 257.91 | 0.0669 | 1.89782 | 29.77 |
| 53.8196 | 168.79 | 0.1506 | 1.70340 | 19.48 |
| 55.0099 | 165.61 | 0.3011 | 1.66933 | 19.12 |
| 62.0610 | 31.67 | 0.1338 | 1.49553 | 3.66 |
| 62.6149 | 129.77 | 0.1673 | 1.48363 | 14.98 |
| 68.6971 | 55.63 | 0.2007 | 1.36636 | 6.42 |
| 70.1959 | 63.55 | 0.1673 | 1.34082 | 7.33 |
| 74.0345 | 12.14 | 0.2007 | 1.28051 | 1.40 |
| 74.9830 | 99.36 | 0.2007 | 1.26665 | 11.47 |
| 75.9788 | 25.24 | 0.2007 | 1.25251 | 2.91 |
| 80.9764 | 4.24 | 0.6691 | 1.18735 | 0.49 |
| 82.6274 | 59.95 | 0.1224 | 1.16680 | 6.92 |

3.3 Difractogram of TiO2/Ag (300/0.93 mg)

## Main Graphics. Analyze View:

## Peak List:

| Pos. [°2Th.] | Height [cts] | FWHM Left [°2Th.] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 25.2592 | 1087.19 | 0.2007 | 3.52594 | 100.00 |
| 36.9089 | 73.77 | 0.2007 | 2.43543 | 6.79 |
| 37.6928 | 246.26 | 0.1224 | 2.38459 | 22.65 |
| 37.7750 | 250.46 | 0.0836 | 2.38156 | 23.04 |
| 38.4671 | 84.06 | 0.2007 | 2.34029 | 7.73 |
| 47.9823 | 366.45 | 0.1004 | 1.89608 | 33.71 |
| 53.7824 | 199.31 | 0.1171 | 1.70449 | 18.33 |
| 55.0057 | 236.11 | 0.0816 | 1.66806 | 21.72 |
| 62.0247 | 35.67 | 0.1673 | 1.49632 | 3.28 |
| 62.6250 | 156.99 | 0.1171 | 1.48341 | 14.44 |
| 68.6572 | 76.40 | 0.1004 | 1.36706 | 7.03 |
| 70.2697 | 82.73 | 0.1171 | 1.33959 | 7.61 |
| 75.0281 | 113.47 | 0.1004 | 1.26600 | 10.44 |
| 75.9904 | 31.86 | 0.1338 | 1.25234 | 2.93 |
| 82.6029 | 57.01 | 0.1338 | 1.16805 | 5.24 |

3.4 Difractogram of TiO2/Ag (450/0.51 mg)

## Main Graphics. Analyze View:

## Peak List:

| Pos. [°2Th.] | Height [cts] | FWHM Left [°2Th.] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 25.1932 | 1204.81 | 0.1338 | 3.53502 | 100.00 |
| 27.3402 | 13.11 | 0.2007 | 3.26211 | 1.09 |
| 36.8265 | 60.20 | 0.2007 | 2.44069 | 5.00 |
| 37.6652 | 265.19 | 0.0669 | 2.38825 | 22.01 |
| 38.4377 | 77.14 | 0.1673 | 2.34201 | 6.40 |
| 47.9267 | 391.90 | 0.0816 | 1.89658 | 32.53 |
| 48.0490 | 266.04 | 0.0816 | 1.89674 | 22.08 |
| 53.7986 | 225.35 | 0.1632 | 1.70260 | 18.70 |
| 54.9364 | 239.77 | 0.1428 | 1.67000 | 19.90 |
| 61.9873 | 48.66 | 0.1224 | 1.49589 | 4.04 |
| 62.5483 | 171.12 | 0.1020 | 1.48382 | 14.20 |
| 68.6414 | 72.92 | 0.1632 | 1.36620 | 6.05 |
| 70.1653 | 88.32 | 0.1020 | 1.34022 | 7.33 |
| 74.8996 | 110.78 | 0.1224 | 1.26680 | 9.19 |
| 75.1727 | 69.64 | 0.1224 | 1.26601 | 5.78 |
| 75.9150 | 31.36 | 0.2448 | 1.25236 | 2.60 |
| 82.5714 | 58.15 | 0.2040 | 1.16745 | 4.83 |

SI 4: Caracterization Result of FTIR

4.1 Spectra of TiO2

4.2 Spectra of TiO2/Ag (150/1.77 mg)

4.3 Spectra of TiO2/Ag (300/0.93 mg)

4.4 Spectra of TiO2/Ag (450/0.51 mg)

SI 5: Measurement result of inhibition zone

Additional information:

Blank disk diameter 	: 6 mm

Sample		: TiO2/Ag (I) with 0.3 g/L of the doses

TiO2/Ag (I) with 0.50 g/L of the doses

TiO2/Ag (I) with 0.7 g/L of the doses

TiO2/Ag (I) with 1 g/L of the doses

Ampicillin	: as a positive control with 10 µg of concentration.

Blank Disk	: as a negative control with aquades.

Fungi for susceptibility test	: Candida albicans.

Test Method	: Agar Disc Diffusion Test (Kirby-Bauer)

Table V.1. The effect of visible light irradiation time and dosage of TiO2/Ag (I) on the antifungal activity of Candida albicans

| Sample Dosages | Irradiation time (hours) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 3 | 5 | 7 | 10 |
|  | Inhibition zone (mm) |  |  |  |  |
| Control (+)* | 24.01 mm | 24.01 mm | 24.01 mm | 24.01 mm | 24.01 mm |
| Control (-)** | 0 mm | 0 mm | 0 mm | 0 mm | 0 mm |
| 0.3 g/L | 1.01 mm | 1.03 mm | 2.05 mm | 1.03 mm | 1.02 mm |
| 0.5 g/L | 1.02 mm | 1.03 mm | 4.05 mm | 1.06 mm | 1.05 mm |
| 0.7 g/L | 1.02 mm | 1.03 mm | 3.02 mm | 1.03 mm | 1.04 mm |
| 1 g/L | 1.02 mm | 1.04 mm | 3.01 mm | 1.04 mm | 1.04 mm |

*ampicillin as a positive control

**aquades as a negative control

Tabel V.2. The effect of UV light irradiation time and dosage of TiO2/Ag (I) on the antifungal activity of Candida albicans

| Sample dosages | Irradiation time (hours) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 3 | 5 | 7 | 10 |
|  | Inhibition zone (mm) |  |  |  |  |
| Control (+)* | 24.00 mm | 24.00 mm | 24.01 mm | 24.01 mm | 24.01 mm |
| Control (-)** | 0 mm | 0 mm | 0 mm | 0 mm | 0 mm |
| 0.3 g/L | 1.03 mm | 1.06 mm | 1.96 mm | 1.24 mm | 1.23 mm |
| 0.5 g/L | 1.05 mm | 1.06 mm | 5.12 mm | 1.25 mm | 1.23 mm |
| 0.7 g/L | 1.02 mm | 1.04 mm | 3.03 mm | 1.22 mm | 1.04 mm |
| 1 g/L | 1.02 mm | 1.04 mm | 3.01 mm | 1.04 mm | 1.04 mm |

*ampicillin as a positive control

**aquades as a negative control

Tabel V.3. The effect of visible light irradiation time and dosage of TiO2 on the antifungal activity of Candida albicans

| Sample Dosages | Irradiation time (hours) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 3 | 5 | 7 | 10 |
|  | Inhibition zone (mm) |  |  |  |  |
| Control (+)* | 24.00 mm | 24.00 mm | 24.00 mm | 24.00 mm | 24.00 mm |
| Control (-)** | 0 mm | 0 mm | 0 mm | 0 mm | 0 mm |
| 0.3 g/L | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm |
| 0.5 g/L | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm |
| 0.7 g/L | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm |
| 1 g/L | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm |

*ampicillin as a positive control

**aquades as a negative control

Tabel V.4. The effect of UV light irradiation time and dosage of TiO2 on the antifungal activity of Candida albicans

| Sample dosages | Irradiation time (hours) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 3 | 5 | 7 | 10 |
|  | Inhibition zone (mm) |  |  |  |  |
| Control (+)* | 24.00 mm | 24.00 mm | 24.00 mm | 24.00 mm | 24.00 mm |
| Control (-)** | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm | 0.00 mm |
| 0.3 g/L | 2.01 mm | 2.01 mm | 2.01 mm | 2.00 mm | 2.00 mm |
| 0.5 g/L | 2.01 mm | 2.01 mm | 2.01 mm | 2.00 mm | 2.00 mm |
| 0.7 g/L | 2.01 mm | 2.01 mm | 2.01 mm | 2.00 mm | 2.00 mm |
| 1 g/L | 2.01 mm | 2.01 mm | 2.01 mm | 2.00 mm | 2.00 mm |

*ampicillin as a positive control

**aquades as a negative control

SI 6: Inhibition zone images of TiO2/Ag photocatalyst on various irradiation treatments

Control (-)

Control (+)

0.7 g/L

1 g/L

0.5 g/L

0.3 g/L

Figure VI.1. Inhibition zone of TiO2/AgNPs (I) on UV light irradiation

for 5 h on the Candida albicans

0.5 g/L

Control (-)

0.7 g/L

1 g/L

0.3 g/L

Control (+)

Figure VI.2. Inhibition zone of TiO2/AgNPs (I) on visible light irradiation

for 5 h on the Candida albicans

SI 6: Inhibition zone images of TiO2 photocatalyst on various irradiation treatments

1 g/L

Control (+)

Control (-)

0.3 g/L

0.7 g/L

0.5 g/L

Figure VI.3. Inhibition zone of TiO2 on visible light irradiation for 5 h on the Candida albicans

0.7 g/L

1 g/L

Control (+)

Control (-)

0.5 g/L

0.3 g/L

Figure VI.4. Inhibition zone of TiO2 on UV light irradiation for 5 h on the Candida albicans

SI 7: EDX Spectra

7.1 EDX Spectra of TiO2

7.2 EDX Spectra of TiO2/Ag (I)

7.3 EDX Spectra of TiO2/Ag (II)

7.4 EDX Spectra of TiO2/Ag (III)